## Slide 2
Yellow LED array here and on tube assy. means X-rays are on
Generator Button Display Generator ready
Enclosure Display Green : Measurement server connected Blue > : Scan in progress White : Measurement server not connected
Bruker d8 Generator and Enclosure Display Settings (left side front of d8)

## Slide 3
Bruker d8 Goniometer Configuration
X-ray tube Cu source
LED indicators Upper red when shutter open Lower yellow when tube on
Sample holder
Lynxeye XE detector
Module A Default: 0.6 mm anti-scatter slit Always use
Module B (left) Default: Ni filter 0.0125 mm Ni filter Cu Kb removal Here empty
Module D Lynxeye Left and Right Left: filter typically empty Right: Soller 2.5 degree slit
Module C Receiving slit / Ni filter No slits are used with Lynxeye
Module B (right) Soller slit 2.5 degrees Always use
Anti-scatter fin Here empty

## Slide 4
Bruker d8 Goniometer Configuration
X-ray tube Cu source
LED indicators Upper red when shutter open Lower yellow when tube on
Sample holder
Lynxeye XE detector
Module A Default: 0.6 mm anti-scatter slit Always use
Module B (left) Default: Ni filter 0.0125 mm Ni filter Cu Kb removal Here empty
Module D Lynxeye Left and Right Left: filter typically empty Right: Soller 2.5 degree slit
Module C Receiving slit / Ni filter No slits are used with Lynxeye
Module B (right) Soller slit 2.5 degrees Always use
Anti-scatter fin Here empty